## Slide 1: Module 4 Design of joints
Lecture 13
Welded connections
Presentation by ….
COMITE INTERNATIONAL POUR LE DEVELOPPEMENT
ET L'ETUDE DE LA CONSTRUCTION TUBULAIRE

## Slide 2: Welded Connections
Welded Connections between Circular Hollow Sections (CHS)
  General Introduction
  Types of joints
  Modes of failure
  Analytical models
  Design models

## Slide 3: Welded Connections
Welded Connections between Rectangular Hollow Sections (RHS)
  General introduction
  Types of joints
  Modes of failure
  Analytical models
  Design models

## Slide 4: Welded Connections
1. Welded Connections between Circular Hollow Sections (CHS)

## Slide 5: General introduction
Circular hollow sections can be connected in various ways
  With special prefabricated connectors (e.g. Mero)
  With end pieces which allow a bolted connection
  Welded to a plate
  Welded directly to the through member (chord)
Simplest solution is to profile the ends of the members which have to be connected to the chord and weld the members directly to each other

## Slide 6: General introduction
Load transfer is rather complex due to the non-linear stiffness distribution along the perimeter of the connected braces
Design rules have been based on simplified analytical models in combination with experimental evidence, resulting in semi-empirical design formulae

## Slide 7: Loading cases
For design there are three loading cases
  Axial load
  Moment in the plane (IPB)
  Moment out of the plane (OPB)
Axial load
Moment in the plane
Moment out of the plane

## Slide 8: Modes of Failure
Various possible failure modes can be expected:
  Brace failure (yielding, local buckling)
  Weld failure
  Lamellar tearing
  Chord plastification (face/wall, or cross section)
  Chord punching shear failure
  Chord local buckling
  Chord shear failure
Color pictures taken from Wardenier, “Hollow sections in structural applications”, 2002

## Slide 9: Modes of Failure
Weld failure
  Excluded by use efficient throat thickness of the welds
Lamellar tearing
  Excluded by material properties
Local buckling of the chord or brace sections
  Excluded by using sections with can be classified to a maximum cross section class 2

## Slide 10: Basic strength formulae
Design resistances for plate to CHS connections are related to a general strength function:
  N1 = f() f() fy0 t0² f(n’)
  where: f() = 5,0 / (1 - 0,81)
  f() = 1 + 0,25 (lower bound value)
  For more details, see CIDECT Design Guide 9, 6.3.1

## Slide 11: Analytical Models
For the determination of the influencing joint parameters, three analytical models are used:
  Ring model (originally developed by Togo)
  Punching shear model
  Chord shear model

## Slide 12: Ring model
Based on the assumption that most of the loading is transferred at the saddles (point A in the next figure) of the brace, since the chord behaves most stiffly at that part of the connection perimeter

## Slide 13: Ring model
Originally developed by Togo (for axial loading)
t0
A
A
B
ti
A
B
A
mp

mp
d0
Be

## Slide 14: Ring model
The load N1 in the brace can be divided into two loads of 0,5·N1·sinΘi perpendicular to the chord in a distance c1·d1 at the saddles.
mp

mp
d0

## Slide 15: Ring model
These loads will be transferred by an effective length Be of the chord
The load 0,5·N1·sini is now considered as a linear distributed load over the effective length Be
Be
mp

mp
d0

## Slide 16: Ring model
At failure, the plastic yield capacity will be reached at the points A and B
Neglecting the influence of axial and shear stresses on the plastic moment mp per unit length, mp results in:
t
0
A
A
B
t
i
A
B
A
i
i
sin
Θ
N

i
i
sin
Θ
N

m
p

m
p
d
0
B
e
2
i
sin
Θ
i
N

2
sin
Θ
N
i
i

i
0
t
d

e
i
i
B
2
sin
Θ
N



## Slide 17: Ring model
With d0-t0≈d0 (neglecting t)
The effective length Be was determined experimentally and depends on the β ratio. An average value is: Be = 2,5d0 – 3,0d0

## Slide 18: Ring model
To take into account the influence of the axial load in the chord the chord pre-stress function f(n’) is used
f(n’) was determined by experiments

## Slide 19: Punching shear model
Caused by the brace load component perpendicular to the chord section N1∙sinΘ1
Punching shear resistance based on the effective punching shear area ∙d1∙t0 multiplied by the punching shear resistance fy / √3

## Slide 20: Punching shear model
For brace angles 1 < 90° the connection perimeter is idealized as an ellipse
Ratio between the perimeter of the ellipse and the circle (for i = 90°) is given by (1+sin1)/(2∙sin1)
Punching shear criterion

## Slide 21: Chord shear model
K-joints with a large width-ratio  may fail by shear failure in the gap location
Chord cross section plastification due to shear, axial load and bending (if present)
For compact chords it can be shown with plastic analysis that the chord shear capacity is:

## Slide 22: Chord shear model (Welded connections between CHS)
Axial load capacity of the chord section
If the bending moments are small, only the interaction between axial and shear load has to be considered:

## Slide 23: Evaluation to design rules
With results of experimental and numerical investigations design models are adapted to EN 1993-1-8 by statistical evaluations of the analytical models

## Slide 24: Range of validity for CHS
Range of validity for welded joints between CHS brace members and CHS chord
For joints within the range of validity only chord face failure and punching shear have to be considered

## Slide 25: Design resistance of welded joints
Chord plastification of CHS connections (T- and Y joints) under axial load

## Slide 26: Design resistance of welded joints
Chord plastification of CHS connections (X-joint) under axial load

## Slide 27: Design axial resistance of welded joints
Chord plastification of CHS connections (K-joint) under axial load

## Slide 28: Design axial resistance of welded joints
Punching shear failure of CHS connections (all types of joints) under axial load

## Slide 29: Design axial resistance of welded joints
Punching shear failure of CHS connections (all types of joints) under axial load
Factors
  kg for consider gap size
  kp for consider chord pre-stressing (for compression kp  1) where: n’ = ratio of the axial design stress Ed to the yield strength fy0

## Slide 30: Joints loaded by bending moments
The design resistance formulae for joints loaded by in plane Mi,p or out of plane bending Mo,p have been determined in a similar way as for axially loaded joints, also resulting in two strength criteria:
  Chord plastification
  Chord punching shear

## Slide 31: Joints loaded by in plane bending moments (IPB)
Chord plastification of joints between CHS brace and chord members
Exemplary for chord face failure for T-, X- and Y-joints

## Slide 32: Joints loaded by bending moments
Punching shear of joints between CHS brace and chord members (all types of joints)

## Slide 33: Design resistances moments of welded joints
Consideration of chord pre-stress
  Factor kp

## Slide 34: Range of validity for CHS
Because the d/t ratios have been limited to cross section class 2 the governing modes of failure to be considered have been reduced to:
  chord plastification
  chord punching shear

## Slide 35: Design of Welds
According to Eurocode 3 the throat thickness a of a fillet weld should satisfy the following requirements:
only for ti  8mm (fillet welds recommended)
  a  0,92 ti for S 235
  a  0,96 ti for S 275
  a  1,10 ti for S 355
  a  1,42 ti for S 420
  a  1,48 ti for S 460
for ti > 8mm (full seam butt welds recommended)
  a = t

## Slide 36: Other types of CHS joints
I, H or RHS sections connected to CHS members
Related joints
Plate to CHS connections
Multiplanar joints

## Slide 37: Design resistances of welded joints
Chord plastification RHS sections connected to CHS members for axial load, IPB and OPB
Exemplary for T-joints

## Slide 38: Design resistances of welded joints
Punching shear failure of I, H or RHS sections connected to CHS members
Range of validity for I, H or RHS sections connected to CHS members

## Slide 39: Related joints
Design resistances of related joints
  DY-joint under axial loading Design resistance from X-joint acc. to EN 1993-1-8
  KT-joint under axial loading Design resistance from K-joint acc. to EN 1993-1-8

## Slide 40: Design resistances of welded joints
Chord plastification of gusset plates connected to CHS members
E.g. T-joints with transverse plate arrangements

## Slide 41: Design resistances of welded joints
Punching shear of gusset plates connected to CHS members
Range of validity of gusset plates connected to CHS members

## Slide 42: Summary of Plate to CHS connections
Design resistance
of welded CHS
joints with gusset
plates
Design resistance of welded CHS and open sections

## Slide 43: Multiplanar joints
For multiplanar joints, two additional effects influence the joint capacity compared to that one for uniplanar joints:
  the geometrical effects (stiffening by the multiplanar joints)
  the loading effects

## Slide 44: Welded Connections
2. Welded Connections between Rectangular Hollow Sections (RHS)

## Slide 45: General introduction
The most economical and common way to connect rectangular hollow sections is by direct connection without any intersecting plates or gussets, this also gives the most efficient way for protection and maintenance
The connections between rectangular hollow sections can be easily made, since the connecting members have to be provided with straight end cuts only

## Slide 46: General introduction
Basic RHS connections
  T-joints
  Y-joints
  X-joints
  K-joints (with gap and overlap)
Combined Connections
  N-joint (with gap and overlap)
  KT-joint (with gap and overlap)

## Slide 47: Modes of Failure
The following modes of failure can occur:
  Brace effective width failure (tension brace or compression brace plastification)
  Weld failure
  Lamellar tearing
  Chord face plastification
  Chord punching shear failure
  Chord side wall yielding or buckling
  Chord local buckling
  Chord shear failure

## Slide 48: Modes of Failure
Failure modes for
welded RHS connections

## Slide 49: Modes of Failure
The following failure modes have to be considered in design:
  Brace effective width failure
  Chord face plastification
  Chord punching shear
  Chord side wall failure
  Chord shear failure

## Slide 50: Analytical Models
For the determination of the influencing joint parameters, five analytical models are used:
  Yield line model
  Punching shear model
  Brace effective width model
  Chord side wall bearing or buckling model
  Chord shear model

## Slide 51: Yield line model
b) Top view
N1
g
a) longitudinal section
h0
b0


N2
b1

li
i


For joints with medium  ratios the yield line model gives a good estimate of the chord face plastification capacity
For high  ratios infinite strength prediction
For small  ratios the deformations may be too high to realise the yield line pattern

## Slide 52: Yield line model
In principle, the yield line method is an upper bound approach
Various yield line pattern have to be examined in order to obtain the lowest capacity
Strain hardening effects and membrane action not considered
Based on equating the external energy by the external force N1 over a deflection  and the internal energy by the plastic hinge system with yield line lengths li and rotation angles i

## Slide 53: Yield line model
N1 sinΘ1  = li I mp
mp = ¼ t0² fy0 (per unit length)
Equating the sum to the external work gives:
This is a minimum for: or

## Slide 54: Yield line model
Substitution gives the capacity (T-,Y- and X-joints):
In this model some simplifications have been incorporated ( thickness of the sections, welds)

## Slide 55: Punching shear model
N1
0,5·be,p
0,5·be,p
h1
sin1
a) Longitudinal cut
b) Top view
a) Cross section
d) very small gap
e) g = b0 – b2
f) big gap
sin2
h2
h1
t0
1

## Slide 56: Punching shear model
Punching shear is caused by the brace load component perpendicular to the chord face
Since of the non-uniform stress distribution at connection and not sufficient deformation capacity may be available, only parts of connection perimeters are effective for punching shear failure
Therefore the punching shear criterion is:

## Slide 57: Punching shear model
For K-gap joints the gap size is extremely important for the effective punching shear length
If the gap size is close to zero and the β value is low to medium, the gap part is relatively too stiff compared to the other perimeter parts
Reduced effective length for punching shear

## Slide 58: Punching shear model
For a large gaps the situation is as for T, Y and X-joints, thus
For a gap where the stiffness is about the same as at the sides of the braces, the punching shear criterion becomes:
e) g = b0 – b2
f) Big gap
sin2
h2

## Slide 59: Punching shear model
Neglecting the brace thickness and the weld sizes, the gap here has to satisfy:
Due to the deformation capacity of the material, which has been proved experimentally, the limit can be extended to
0,5 (1-β) ≤ g/b0 ≤ 1,5 (1-β)

## Slide 60: Brace effective width model
N1
h1
0,5·beff
1
Similar to punching shear failure but the complete brace load has to be taken into account
For a T, Y and X joint, the effective width criterion is:
N1 = fy1 t1 (2h1+2be– 4t1)
As for punching shear failure the gaps are extremely important for the effective lengths

## Slide 61: Brace effective width model
For K-joints with gaps in the allowed range the brace effective width criterion is N2 = fy2 t2 (2h2+b2+be– 4t1)
No regulations for small gaps available
For big gaps the criterion for T-, Y- and X-joints can be used

## Slide 62: Chord side wall bearing or buckling model
T, Y and X joints with a high  ratio generally fail by yielding or buckling of the chord side walls
For joints with  = 1,0 the yield capacity of the chord webs can be determined by:
For slender walls the yield stress fy0 is replaced by a buckling stress fk which is obtained from the European buckling curve a for a Euler-Strut with a buckling length of h0-3t
N1
b) Cross cut
h1
t0
1
2,5·t0
2,5·t0
h1
sin1
+5t0
b1
t1
b0
a) Longitudinal cut
h0
t0

## Slide 63: Chord shear model
Resistance based on the basic formulae for plastic design
M
M
V
V
Ni,Rd
N0,gap
N0,gap
AV
g
h0
b0
t0
1

## Slide 64: Chord shear model
The plastic shear load capacity is:
with an effective shear area of AV = (2h0 + α ∙ b0) t0
AV
h0
b0
t0

## Slide 65: Chord shear model
Based on the Huber Hencky-Von Mises criterion the following interaction formula can be determined:

## Slide 66: Design axial resistances of welded joints
Chord face plastification of square or circular braces connected RHS chords under axial load
In this case the type of joints are T-, Y- and X-joints

## Slide 67: Design axial resistances of welded joints
Effective widths for punching shear be.p and brace failures beff
Factor kn for consideration of chord pre-stress

## Slide 68: Joints between circular braces and a rectangular chord
As far as chord face plastification concerns the joint strength of a joint with a circular hollow section brace diameter d is about /4 times that of a joint with a square hollow section brace with a width bi = di
This means that the same formulae can be used as for square hollow section joints, but they have to be multiplied by /4

## Slide 69: Design axial resistances of welded T,X and Y joints
Other Failure modes of square or circular braces connected RHS chords (for T-, Y- and X-joint) under axial load

## Slide 70: Design axial resistances of welded T,X and Y joints
Normalised buckling length, effective width be.p and beff and chord pre-stress consideration kn

## Slide 71: Design axial resistances of welded K and N joints
Determination of the effective shear area

## Slide 72: Joints loaded by bending moments
The design resistances are derived in a similar way as for the axially loaded joints
To simplify the design, also here limitations are given for the range of validity to limit the criteria to be checked
For Vierendeel girders it is recommended to choose joints with = 1,0 to provide sufficient stiffness and strength

## Slide 73: Design resistances moments (IPB) of welded joints
RHS braces connected to RHS chords (T- and X-joints) under moment loading (exemplary for IPB)

## Slide 74: Design resistances moments of welded joints
Effective widths be.p and beff and factor kn for considering chord pre-stress for RHS braces connected to RHS chords under moment loading

## Slide 75: Other types of joints or other load conditions
Gusset plates, I- or H-sections connected to RHS members
Multiplanar Joints

## Slide 76: Joints between plates or I sections and RHS chords
These connections are considered similar to rectangular hollow section joints and the same modes of failure have to be considered

## Slide 77: Design resistances of welded joints
Gusset plates (longitudinal arrangement) to RHS members under axial load

## Slide 78: Design resistances of welded joints
I- or H-sections to RHS members under axial load

## Slide 79: Design resistances of welded joints
Range of validity of gusset plates, I- or H-sections to RHS members

## Slide 80: Design resistances of welded joints
Effective widths be.p and beff and factor km for considering chord pre-stress for Gusset plates, I- or H-sections to RHS members

## Slide 81: Multiplanar Joints
Similar to circular hollow section joints, compared to uniplanar joints, multiplanar joints have a geometrical effect and a loading effect to be considered
A multiplanar brace has a geometrical influence only if the value is large, because then the chord side wall is stiffened