- Module 7

Worked examples

Lecture 20Fatigue in lattice girder joint

- Contents:

1.	Introduction

2.	Actions

3.	Applicability of method

4.	Effect of secondary bending moments in the joint

5.	Partial safety factors

6.	Fatigue assessment

7.	Cumulative damage

8.	References

| - Introduction |  |
| --- | --- |
| This worked example deals with the fatigue verification of a welded “N” joint node that is part of a lattice girder (reference to the overlapping joint of previous Lecture 19 is made here, so that square hollow section members are of concern). Figure 1 gives the studied joint configuration. A square hollow section RHS 140x140x8 are used for both the diagonal and vertical braces, while RHS 180x180x8 are used for the chord. An overlap of 90 mm is considered. Steel grade S355 is adopted. |  |
| - Overlapping “N” joint |  |
| The fatigue design check procedure has to be performed for all elements requiring a fatigue design check in the node, i.e. the vertical and diagonal braces and the chord. For sake of illustration, only the diagonal brace is checked hereafter. |  |
| - Actions |  |
| The damage tolerant assessment method is followed here. Table 1 reports on the assumed nominal stress ranges and associated number of cycles during the specified life of the structure. |  |
| - Fatigue stress spectra |  |
| Nominal stress range; Number of cycles. 1 = 70 N/mm2; n1 = 1104. 2 = 50 N/mm2; n2 = 1105. 3 = 30 N/mm2; n3 = 1105. |  |
| - Applicability of method |  |
| According to Eurocode 3 Part 1.9 Table 8.7, the relevant detail category is 50 with m = 5, since t0 / ti = 8 mm / 8 mm = 1,0. |  |
| For the application of the method to be valid, one has to check if the following conditions are met: |  |
| No out-of-plane eccentricity eo/p is present. |  |
| Since all conditions are fulfilled, the method applies. |  |
| - Effect of secondary bending moments in the joint |  |
| The effect of secondary bending moments due to the stiffness of the connetion is accounted for by means of so-called k1-factors. Eurocode 3 Table 4.2 leads to k1 = 1,4 for the diagonal brace. It is here implicitly assumed that the modelling of the lattice girder has been based on a simplified truss model with pinned connections for the braces and continuous chords. |  |

| - Partial safety factors |  |
| --- | --- |
| Assuming that the structure is checked according to the damage tolerant method and that the consequence of failure is high, the partial safety factor for fatigue strength is taken as Mf = 1,15. |  |
| Besides this, the partial safety factor for lading is chosen as Ff = 1,0. |  |
| - Fatigue assessment |  |
| The reference fatigue strength corresponding to 2106 cycles for the detail category 50 is c = 50 N/mm2. The fatigue strength curve for lattice girders has a constant slope m = 5 and the number of stress fluctuations corresponding to a nominal stress range i is: |  |
| Therefore, the following Ni values of Table 2 have been obtained: |  |
| - Determination of the number of stress fluctuations |  |
| Nominal stress range; Endurance. 1 = 70 N/mm2; N1 = 3,44104. 2 = 50 N/mm2; N2 = 1,85105. 3 = 30 N/mm2; N3 = 2,38106. |  |
| - Cumulative damage |  |
| The partial damage Dd,i caused by ni cycles of stress range i is equal to: |  |
| Consequently, the following partial damages are calculated: |  |
| so that the cumulative damage during the design life is: |  |
| Accordingly, the calculated design life of the diagonal brace is higher than the required design life. |  |
| It is to be noted that the procedure described above shall also be repeated for the other elements requiring a fatigue design check. |  |

- References

- EC3: EN 1993-1-9: Eurocode 3: Design of Steel Structures – Part 1.9: Fatigue. CEN, Brussels, May 2005.