## Slide 1: Module 4 Design of joints
Lecture 12
Generalities on joint design
Presentation by ….
COMITE INTERNATIONAL POUR LE DEVELOPPEMENT
ET L'ETUDE DE LA CONSTRUCTION TUBULAIRE

## Slide 2: General introduction
Joint parameters:
Color pictures taken from Wardenier, “Hollow sections in structural applications”, 2002

## Slide 3: General introduction
Joint parameters: The geometry of a particular joint is also generally defined by the non-dimensional joint para- meters α, β, ,  and g‘

## Slide 4: General introduction
For a proper understanding of the behaviour of tubular joints or welded connections between hollow sections it is important to consider
  the load path
  the internal stiffness distribution in a connection
  the material properties

## Slide 5: Load path
The load path shows what parts the loads have to pass and where failure may occur.
The load has to pass the following parts:
  plate
  weld
  hollow section face (through thickness)
  hollow section side wall
Thus, in principle failures can occur in these parts.

## Slide 6: Internal stiffness distribution
The stiffness distribution in the joint determines the elastic stress distribution.
Consider the stiffness of the plate and the connected face of the hollow section.
The resulting elastic stress pattern in the plate can be determined in two ways:
  Consider the deformations under a uniform stress
  Assume rigid plate

## Slide 7: Internal stiffness distribution
Elastic stress distribution in an X-joint
t0
ti
d0
di
Θi

## Slide 8: Effect of material properties
Important for static design is
  yielding
  deformation capacity

## Slide 9: Failure modes
the possible failure modes for the plate to RHS connection of this example will be considered:

## Slide 10: Failure modes
1. Plate
  If the chord width-to-thickness ratio bo/to is low and the material has sufficient ductility, the yield capacity of the plate can be reached
2. Welds
  If the strength of the fillet welds is lower than that of the plate, the welds may fail
  Generally it is recommended that the welds should preferably be designed to be stronger than the connected elements

## Slide 11: Failure modes
3. Chord face
  Especially for thick material, cracking can occur due to MnS inclusions, called lamellar tearing
  If b1 < bo, other failure modes can be obtained for the chord, i.e.: top face plastification or chord punching shear
  Punching shear of the hollow section face can only occur if the plate width b1 is smaller than bo-2to

## Slide 12: Failure modes
4. Chord side wall
  All the stresses have to be transmitted through the side walls over a limited width, thus this may be a critical failure mode
  If the loading is compression instead of tension, the stability of the side wall may be critical

## Slide 13: General failure criteria
(1)
(1)
(2)
In general, the static strength can be characterized by various criteria, i.e.:
  ultimate load resistance (1)
  3%d0 deformation limit (2)
  (visually observed) crack
  initiation
compression
tension

## Slide 14: Types of planar CHS joints
Basic joints
  T-joint
  Y-joint
  X-joint
  K-joint (with gap or overlap)
Combined joints
  N-joint (with gap or overlap)
  KT-joint (with gap or overlap)

## Slide 15: Types of planar RHS joints
Welded RHS connections
  T-joints
  Y-joints
  X-joints
  K-joints (with gap and overlap)
Combined joints
  N-joint (with gap and overlap)
  KT-joint (with gap and overlap)

## Slide 16: General failure modes
Various failure modes for a K-joint of rectangular hollow sections:
  plastification of the chord face
  chord punching shear
  brace failure (effective width)
  chord shear failure
  local buckling of the compression brace
  local buckling of the chord
If the welds are not strong enough, weld failure can also occur or if the material does not have sufficient through thickness properties (TTP) lamellar tearing is possible.

## Slide 17: General failure modes (RHS)
Plastification of the chord face

## Slide 18: General failure modes (RHS)
Chord punching shear

## Slide 19: General failure modes (RHS)
Brace failure (effective width)

## Slide 20: General failure modes (RHS)
Chord shear failure

## Slide 21: General failure modes (RHS)
Lokal buckling of the compression brace

## Slide 22: General failure modes (RHS)
Local buckling of the chord

## Slide 23: General failure modes (RHS)
Weld failure (left) and lamellar tearing (right)

## Slide 24: Range of validity for CHS
c1/t1 limits for the compression brace or limits for efficiency to avoid local buckling of the compression members
Maximum width to thickness ratios for compression parts (Table 5.2 EN 1993-1-1)

## Slide 25: Range of validity for CHS

## Slide 26: Range of validity for CHS

## Slide 27: Design of Welds
The simplified method for design resistance of a fillet weld according to Eurocode 3 (EN 1993-1-8, 4.5.3.3)
The design resistance of a fillet weld may be assumed to be adequate if, at every point along its length, the resultant of all forces transmitted by the weld satisfy the following criterion
where: Fw,Ed = design value of the weld force per unit length
Fw,Rd = design weld resistance per unit length