## Slide 2: Steel stress-strain curves at high temperatures
Steel softens progressively from 100-200°C up.
Only 23% of ambient-temperature strength remains at 700°C.
At 800°C strength reduced to 11% and at 900°C to 6%.
Melts at about 1500°C.
Strain (%)
0.5
1.0
1.5
2.0
Stress (N/mm2)
0
300
250
200
150
100
50
20°C
200°C
300°C
400°C
500°C
600°C
700°C
800°C

## Slide 3: Concrete stress-strain curves at high temperatures
Concrete also loses strength and stiffness from 100°C upwards.
Does not regain strength on cooling.
High temperature properties depend mainly on aggregate type used.

## Slide 4: The fire triangle
Fuel + Oxidant = Combustion products + Energy
CH4 + O2 = CO2 + 2H2O + E
Reaction occurs when Oxygen/fuel mixture hot enough
Heat
Oxygen
Fuel

## Slide 5: Stages of a natural fire - and the standard fire test curve

## Slide 6: The EC1 (ISO834) standard fire curve

## Slide 7: Different EC1 time-temperature curves
Fire resistance times based on standard fire curve - NOT on survival in real fires.
EC1 Parametric Fire temperature-time curves. Based on fire load and compartment properties (< 500 m2). Only allowed with calculation models.

## Slide 8: Time-equivalence
Matches times to given temperature of the element in a natural fire and in Standard Fire.
Used to rate fire severity or element performance relative to furnace test.

## Slide 9: Furnace tests on structural elements
Fire Testing
Load kept constant, fire temperature increased using Standard Fire curve.
Maximum deflection criterion for fire resistance of beams.
Load capacity criterion for fire resistance of columns
Problems
Limited range of spans feasible, simply supported beams most of the time.
Effects of continuity ignored. Beams fail by “run-away”.
Restraint to thermal expansion by surrounding structure ignored.

## Slide 10: Standard fire resistance furnace test

## Slide 11: Standard fire resistance furnace test

## Slide 12: Structural fire protection
Passive Protection
Insulating Board
  Gypsum, Mineral fibre, Vermiculite.
  Easy to apply, aesthetically acceptable.
  Difficulties with complex details.
Cementitious Sprays
  Mineral fibre or vermiculite in cement binder.
  Cheap to apply, but messy; clean-up may be expensive.
  Poor aesthetics; normally used behind suspended ceilings.
Intumescent Paints
  Decorative finish under normal conditions.
  Expands on heating to produce insulating layer.
  Can now be done off-site.

## Slide 13: Inherent fire protection to steel beams

## Slide 14: Steel stress-strain curves at high temperatures
Strength/stiffness reduction factors for elastic modulus and yield strength (2% strain).
Elastic modulus at 600°C reduced by about 70%.
Yield strength at 600°C reduced by over 50%.

## Slide 15: Degradation of steel strength and stiffness
Strength and stiffness reductions very similar for S235, S275, S355, S420 and S460 structural steels and hot-rolled reinforcing bars. (SS)
Cold-worked reinforcing bars S500 deteriorate more rapidly. (Rft)

## Slide 16: Degradation of concrete strength and stiffness
Strength reduction factors
Accurate for normal density concrete with siliceous aggregates.
Conservative for normal density concrete with calcareous aggregates
Conservative for light-weight concretes. All types treated the same.

## Slide 17: Thermal expansion of steel and concrete
Steel thermal expansion stops during crystal structure change in the 700-800°C range.
Concrete unlikely to reach 700°C in time of a building fire.
Light-weight concrete treated as having uniform thermal expansion coefficient.

## Slide 18: Other steel thermal properties

## Slide 19: Establishing Fire Resistance: Strategies

## Slide 20: Establishing fire resistance: the simple process

## Slide 21: Minimum fire resistance periods - UK Building Regulations

## Slide 22: Establishing fire resistance: the simple process

## Slide 23: Load reduction factor in fire
Relative to ambient-temperature design resistance
Either …..
Relative to ambient-temperature design load (more conservative)
Or more usefully…..

## Slide 24: EC3 partial safety factors
In Fire limit state

GA
= 1,0
Permanent loads; accidental design situations

1,1
= 0,5
Combination factor; variable loads, offices
Note:

2,1
is now recommended in
EN 1991
-
1
-
2
Ambient temperature strength design

G
= 1,35
Permanent loads;

Q,1
= 1,5
Variable loads
Q
k.1
/G
k
1
2
3
4

fi
0,53
0,46
0,43
0,41
Q
k,1
/G
k
1
2
3
4

fi
0,53
0,46
0,43
0,41

## Slide 25: Establishing fire resistance: the simple process

## Slide 26: Member classification in fire

## Slide 27: Establishing fire resistance: the simple process

## Slide 28: The “Degree of Utilisation”
0
.
d
.
fi
d
.
fi
0
R
E


…
…
is the design loading of a member in fire









1
M
fi
.
M
fi
0




A simple version of
A simple version of
Degree of Utilisation:
Degree of Utilisation:









1
M
fi
.
M
fi
0




A simple version of
A simple version of
Degree of Utilisation:
Degree of Utilisation:

can be used when no chance
of overall or lateral
-
torsional
buckling
…

conservative if

fi
calculated
as proportion of
design
design
loading
loading
at ambient
temperature.
For steel, material partial safety factors

M1
=1,0

M.fi
=1,0
as a proportion of its resistance at ambient
temperature (t=0) but including material
safety factors for the fire limit state.

## Slide 29: Establishing fire resistance: the simple process

## Slide 30: Critical temperatures of steel members
Based on Standard Fire curve. Simple members only.
Non-slender sections (Classes 1, 2, 3 treated the same.
Slender (Class 4) sections treated conservatively (350°C), or see Annex E of EC3 Part 1-2.

## Slide 31: Establishing fire resistance: the simple process

## Slide 32: Section factor Am/V - unprotected steel members

## Slide 33: Section factor Am/V - inherently protected systems

## Slide 34: Section factor Am/V - hollow sections exposed on all sides

## Slide 35: Establishing fire resistance: the simple process

## Slide 36: Temperature increase of unprotected steel
Temperature increase in time step t:
Heat flux hnet.d has 2 parts:
Radiation:
Convection:

## Slide 37: Establishing fire resistance: the simple process

## Slide 38: Section factor Ap / V - protected steel members

## Slide 39: Section factor Ap / V - hollow sections exposed on all sides

## Slide 40: Establishing fire resistance: the simple process (protected steel)

## Slide 41: Temperature increase of unprotected steel
Some heat stored in protection layer
Heat stored in protection layer relative to heat stored in steel
Temperature rise of steel in time increment t

## Slide 42: Establishing fire resistance: the simple process (protected steel)

## Slide 43: Adaptation factors - beam with concrete slab on top flange

## Slide 44: Unrestrained beams

## Slide 45: Compression members of Class 1, 2 or 3

## Slide 46: Design example

## Slide 47: Tension member: strength design

## Slide 48: Tension member: critical temperature
114
kN
114
kN
Design resistance at 20
°
C, using fire safety factors:
(4.2.3.1)
N
fi.20.Rd
=
1067 x 275 = 293,43
kN
Critical temperature:
Degree of utilisation

0
=
N
fi.d
/ N
fi.20.Rd
114 / 293,43 = 0,39
(4.2.4.2) or (Table 4.1)
Critical temperature

c
= 624
°
C
Design loading in fire:
N
fi.d
(2.4.2.1)
Combination factor,

1.1
= 0,5
N
fi.d
=


kN

## Slide 49: Tension member: fire resistance time

## Slide 50: Tension member: fire protection

## Slide 51: Steel beam: strength design
Section Classification:
Coefficient

= ( 235 /
f
y
)
0,5
= 0,92
Compression
flange
:
c
/
t
= (150
–
3 x12)/12 = 9,5
< 0,85 x 33 x 0,92 = 25,80
Web:
c
/
t
= (250
–
3x12)/12 = 17,8 < 0,85 x 72 x 0,92 = 56,3
The section is
therefore
Class 1.
Applied bending moment:
M
Ed
= 49,59x52/8
= 154,97 kNm
49,59
kN/m
250/150/12
5m
49,59
kN/m
250/150/12
5m
Try RHS 25015012

## Slide 52: Steel beam: strength design

## Slide 53: Steel beam: design resistance at 20°C
Design resistance at 20°
C, using fire safety factors:
For a Class 1 beam
with uniform temperature distribution
,
M
fi.20.Rd
= 658.000 x 275 = 180,95kNm
22,8
kN/m
Design loading in fire:
M
fi.d
Combination factor

1.1
= 0,5
M
fi.d
= (1.9 + 0,5 3,8) 6 52
/8 = 71,25
= 71,25 kNm

## Slide 54: Steel beam: critical temperature
For a beam supporting a concrete
slab
on top flange:
4.2.3.3
M
fi.t.Rd
= M
fi.

.Rd
/

1

2

1
= 0,7

2
= 1,0
M
fi.t.Rd
= 180,95/(0,7x1,0)
= 258,5 kNm
Critical Temperature of the Beam:
4.2.4
.2 or
Degree of utilisation

0
= 71,25 / 258,5 = 0,276
Table 4.1
Critical temperature of beam

cr
= 676
°
C
71,25
kN/m
22,8
kN/m

## Slide 55: Steel beam: fire resistance time

## Slide 56: Steel beam: fire protection

## Slide 57: Steel column: strength design
3,5m
150/150/12
991,8
kN
3,5m
150/150/12
991,8
kN
991,8
kN
Compression Resistance:
Slenderness

= 3,5 / 0,0544 = 64,3

1
= 86,8
Normalised
slenderness = 64,3/86,8 = 0,74
Reduction factor (curve c for cold formed sections),

= 0,70

A
= 1 for Class 1 sections;

M1
= [1,0]
Buckling resistance
N
b.Rd
=


A
A
f
y
/

M1
= 1157
kN
> 991,8
... therefore OK.
Design Loading:
N
Ed
= 991,8 kN
Try RHS 15015012
Section Classification in the fire situation:

= (235/f
y
)
0,5
= 0,92
c /
t
w
= (150
–
2 (12+24)) / 12 = 6,5
< 33
.
0,92 0,85 = 25,81
…
Class 1

## Slide 58: Steel column: design resistance at 20°C
456
kN
456
kN
Design loading in fire:
N
fi.d
N
fi.d
=
(1,9 + 0,5 x 3,8) x 5 x 6 x 4
= 456
kN
N
b,fi,t,Rd
=

fi
A
k
y.
q
max
f
y
/

M.fi
Effective length factor = 0,7 for lowest storey
with pinned base ( intermediate storey would
have 0,5).
Note: this is a favourable effect.
=> Slenderness

= 0.7 x 64,3 = 45

## Slide 59: Steel column: design resistance in the fire situation
FIRST ITERATION
Assume that 1 in the fire situation=
0,85
x 86,8 = 73,78
Note: this is an unfavourable effect (
E
decreasing faster then
f
y
)

Normalised slenderness in the fire situation:

/

1
= 45/73,78 = 0,61
Reduction factor in fire,

fi
= 0,67
EC3: 4.2.3.2 (2)
N
b.fi.0.Rd
= 0,67 
6100 
1 
0,275 / 1 = 1124
kN
Degree of utilization,

0
= 456 / 1124 = 0,406
Critical temperature

cr
= 617
°
C
=> K
E
= 0,279;
K
fy
= 0,210; (0,210/0,279)
0,5
= 0,868

## Slide 60: Steel column: design resistance in the fire situation
SECOND ITERATION

1
in the fire situation=
(
0,85)
0,868
x 86,8 =
(73,78)
75,34


/

1
= 45/75,34 =
(0,61)
0,597
Reduction factor in fire,

fi
=
(0,67)
0,679
EC3: 4.2.3.2 (2)
N
b.fi.0.Rd
= 0,679 
6100 
1 
0,275 / 1 =
(1124)
1139
kN
Degree of utilization,

0
= 456 / 1139 =
(0,406)
0,400
Critical temperature

cr
= 620
°
C (

617
°
C)

## Slide 61: Steel column: design resistance in the fire situation
Note: Working in the load domain, that means calculating the load
bearing capacity in the fire situation after a certain required time
e.g. 30 minutes, would not imply any iteration.

## Slide 62: Steel column: critical temperature, fire resistance time