- Module 4

Design of joints

Lecture 13Welded connections

- Contents:

1.	Different kind of trusses

2.	Trusses analysis

3.	Effective length for compression members

3.1.	Effective length (KL) recommendations

3.1.1.	Simplified rules

4.	Welded Connections between Circular Hollow Sections (CHS)

4.1.	Modes of Failure

4.2.	Analytical Models for axial load connections made of CHS

4.2.1.	Ring model

4.2.2.	Punching shear model

4.2.3.	Chord shear model

4.3.	Basic strength formulae

4.4.	Evaluation to design rules

4.5.	Range of validity for CHS

4.6.	Joints loaded by bending moments

4.7.	Other types of joints made of CHS

4.7.1.	Related joints

4.7.2.	Plate to CHS connections

4.7.3.	Multiplanar joints

5.	Welded Connections between Rectangular Hollow Sections

5.1.	Modes of Failure

5.2.	Analytical Models for axial load connections made of RHS

5.2.1.	Yield line model

5.2.2.	Punching shear model

5.2.3.	Brace effective width model

5.2.4.	Chord side wall bearing or buckling model

5.2.5.	Chord shear model

5.3.	Basic strength formulae

5.4.	Evaluation to design rules

5.5.	Joints loaded by bending moments

5.6.	Other types of joints or other load conditions

5.6.1.	Joints between circular braces and a rectangular chord

5.6.2.	Joints between plates or I sections and RHS chords

5.6.3.	Multiplanar Joints

6.	References

| - Different kind of trusses |  |
| --- | --- |
| - Warren trusses |  |
| - Pratt trusses |  |
| - Fink truss |  |
| The warren trusses (Figure 1) provide the most economical solution because of there long compression brace members. They have round about half of the member of bracing members and half the member of connections compared to Pratt trusses (Figure 2). This results in a lower labour and saves money. |  |
| Truss depth is determined in relation to the span, loads, maximum deflection etc. with increased truss depth reducing the loads in the chord members and increasing the length of the bracing members. |  |
| An ideal span to depth ratio is usually between 10 and 15. A ratio near 15 will represent the optimum value. |  |
| - Trusses analysis |  |
| In the elastic analysis of RHS trusses is assuming that all members are pin connections. |  |
| Nodal eccentricities should be kept in the limits from the following Figure 4. |  |
| - Nodal eccentricities (Wardenier 2002) |  |
| The primary bending moments, produced by these eccentricities need to be taken into account when the compression chord is treating as a beam column. |  |
| The moments due to eccentricity can be ignored for the design of chords under tensile loading and for the brace members. For chords under compressive loading they have to be considered. |  |
| If moments are distributed to the bracing members, the connection capacity must than be checked for the interaction between axial load and bending moments for each bracing member. |  |
| A rigid joint frame analysis is not recommended for most planar directly welded trusses, as it tends to exaggerate bracing member moments, and the axial force distribution will be still similar to that for a pin-joint analysis. |  |
| Transverse loads produce primary moments which must be taken into account when designing the chord. |  |
| The following table summarizes when moments have to be considered for designing an RHS truss. |  |
| - Moments need to be considered for RHS truss design (CIDECT Design Guide) |  |
| Type of moment; Primary; Primary; Secondary. Moments due to:; Nodal eccentricity; Transverse member loading; Secondary effects such as local deformations. Compression chord design; Yes; Yes; No. Design of other members; No; Yes; No. Design of connections; No, provided eccentricity limits are not exceeded; Yes, influences f(n); No, provided parametric limits of validity are met. |  |
| Secondary moments, resulting from end fixity of the bracing members to a flexible chord wall, can be ignored for both members and connections provided that there are sufficient deformation and rotation capacity adequate to redistribute stresses after some yielding at the connection. |  |
| This is given when geometric limits of validity are followed. |  |
| - Effective length for compression members |  |
| For compression chords the effective length factor K can always be taken as K = 1,0. In the unlikely situation that all compression members are proportioned on the basis of a single load combination, and all reach the compressive resistance at approximately the same truss loading, an effective length factor K = 1,0 is recommended but generally K is less than 1,0. |  |
| - Effective length (KL) recommendations |  |
| - Simplified rules |  |
| RHS chord member: |  |
| - In the plane of the truss KL = 0,9 L, L is the length between the chord panel points; - In the plane perpendicular to the truss KL = 0,9 L, L is the distance between points of lateral support for the chord. |  |
| RHS or CHS bracing members: |  |
| - In all planes KL = 0,75 L, L is the panel point to panel point length of the member |  |
| The values of K are only valid for RHS members who are connected around the full perimeter of the member, without cropping or flattening of the members. |  |
| - Welded Connections between Circular Hollow Sections (CHS) |  |
| Circular hollow sections can be connected in various ways: |  |
| - With special prefabricated connectors (e.g. Mero); - With end pieces which allow a bolted connection; - Welded to a plate; - Welded directly to the through member (chord). |  |
| Simplest solution is to profile the ends of the members which have to be connected to the chord and weld the members directly to each other. |  |
| The load transfer is rather complex due to the non-linear stiffness distribution along the perimeter of the connected braces. |  |
| Design rules have been based on simplified analytical models in combination with experimental evidence, resulting in semi-empirical design formulae. |  |
| For design there are three loading cases: |  |
| - Axial load; - Moment in the plane; - Moment out of the plane; |  |
| In Lecture 13 mainly axial loaded joints are discussed. For detailed information on moment loading of hollow section connections it should be referred to Wardenier 2002. |  |
| - Modes of Failure |  |
| Various possible failure modes can be expected: |  |
| - Brace failure (yielding, local buckling); - Weld failure; - Lamellar tearing; - Chord yielding (face/wall, or cross section); - Chord punching shear failure; - Chord local buckling; - Chord shear failure. |  |
| - Failure modes for axial loading and in-plane bending (EC1993-1-8:2003) |  |
| Weld failure: |  |
| - Excluded by use efficient throat thickness of the welds. |  |
| Lamellar tearing: |  |
| - Excluded by using materials with material properties according to technical delivery standards (EN 10210:2006 and EN 10219:2006). |  |
| Local buckling of the chord or brace sections: |  |
| - Excluded by using sections which can be classified to a maximum cross section Class 2. |  |
| - Analytical Models for axial load connections made of CHS |  |
| For the determination of the influencing joint parameters, three basic analytical models are used for hollow section joints made of CHS: |  |
| - Ring model; - Punching shear model; - Chord shear model. |  |
| - Ring model |  |
| The ring model was originally developed by Togo. Based on the assumption that most of the loading is transferred at the saddles (point A in Figure 6) of the brace, since the chord behaves most stiffly at that part of the connection perimeter. |  |
| In Figure 6 the ring model for axial loading is shown. |  |
| - Togo’s ring model for axial loading |  |
| The load Ni in the brace can be divided into two loads of 0,5 Ni sini perpendicular to the chord in a distance (di - ti) = c1 di at the saddles. |  |
| These loads will be transferred by an effective length Be to the chord. |  |
| The load 0,5·Ni·sini is now considered as a line load over the effective length Be. |  |
| At failure, the plastic yield capacity mp will be reached at the points A and B. |  |
| Neglecting the influence of axial and shear stresses on the plastic moment mp per unit length, mp results in: |  |
| With d0 – t0 ≈ d0 (neglecting t). |  |
| The effective length Be was determined experimentally and depends on the  ratio. An average value is: Be = 2,5 d0 – 3,0 d0. |  |
| - Punching shear model |  |
| For punching shear failure, the brace is pulling out the chord section. The failure is caused by the brace load component perpendicular to the chord section Ni sini. |  |
| The punching shear resistance for connections with a brace angle of i = 90° can be calculated using the effective punching shear area  d1 t0 (simplified as perimeter of the according brace multiplied by the chord thickness) and the punching shear resistance . Thus: |  |
| For brace angles different from i = 90°, the connection perimeter can be idealized as an ellipse. |  |
| Since the perimeter of an ellipse cannot been calculated analytically, the ratio between the perimeter of the ellipse (for i < 90°) and the circle (for i = 90°) is given simplified by (1 + sin i) / (2 sin i). Thus, the punching shear criterion is: |  |
| - Chord shear model |  |
| In T-joints the failure is governed by a combination of the local failure of the chord cross section due to the brace loads perpendicular to the chord and chord failure due to shear, bending and, if present, the axial loading of the chord. |  |
| K-joints with a large width-ratio  may fail by shear failure in the gap location. The failure mode is a chord cross section yielding due to shear load, axial load and, if present, bending. |  |
| For compact chords it can be shown with plastic analysis that the chord shear capacity is given by: |  |
| The axial load capacity of the chord section is given by: |  |
| If the bending moments are small, only the interaction between axial and shear load has to be considered: |  |
| - Basic strength formulae |  |
| The analytical ring model has been used as a basis for the determination of the basic joint strength formulae (Eq. ). |  |
| Based on experimental test results for X-joints, c0: |  |
| and c1 (see Eq. had been determined to obtain the function for the mean strength. |  |
| Due to the fact that for T, Y, K and N joints the load transfer is more complicated, functions for  and  had been determined experimentally as well as the function for the gap g resulting in a general presentation: |  |
| In the comparison of the test results with the resulting formulae it had been shown that within the range of validity given (see Table 3) the results can be described by a basic joint strength function for chord yielding with a check for punching shear. The chord shear criterion did not have to be checked separately. |  |
| The chord pre-stress function f(n’) has been investigated separately. Initially, separate functions existed for X and K joints. In the evaluation to design rules by the international committees of IIW-XV-E and the CIDECT Project Group, this has been simplified to one function based on the chord stress o,Ed caused by the pre-stressing load Nop. Since this function is still based on the pre-stress which is in contradiction with the function for joints with square hollow sections, which is based on the maximum chord stress, this item is still under investigation. |  |

| - Evaluation to design rules |  |
| --- | --- |
| In the analysis for the basic joint strength formulae, functions for predicting the mean strength with the lowest coefficient of variation have been determined. |  |
| Considering the scatter in test results, typical tolerances in dimensions and workmanship and the variation in yield stress, characteristic joint strength formulae have been determined with a 5% probability of lower strength. |  |
| These characteristic formulae have been divided by a partial safety factor γM5 = 1,0 and somewhat simplified to derive the design resistance formulae given in the IIW recommendations, the CIDECT design guide and EN 1993-1-8. These formulae have now been adopted in many national recommendations. |  |
| Table 2 shows the design resistance formulae. As shown, the chord yielding criterion and the general punching shear criterion have to be checked. It is also noted that the formula for X-joints fully agrees with Eq based on the ring model. |  |
| - Design resistance of welded joints between CHS (Wardenier 2002) |  |
| - Range of validity for CHS |  |
| Since the design models are calibrated using experimental results, the range of validity has to be limited to the investigated parameter ranges (Table 3). For joints within the range of validity given in Table 3, only chord face failure and punching shear need to considered. |  |
| - Range of validity for hollow section connections made of CHS (EN 1993-1-8) |  |
| Because the d / t ratios have been limited to cross-section Class 2 the governing modes of failure to be considered can be reduced to: |  |
| - Chord yielding; - Chord punching shear. |  |
| - Joints loaded by bending moments |  |
| The design resistance formulae for joints loaded by in-plane Mi.p or out-of-plane bending Mo.p have been determined in a similar way as for axially loaded joints, also resulting in two strength criteria: |  |
| - Chord yielding; - Chord punching shear. |  |
| The basic analytical models are similar to axial loaded joints, but due to the more complicated load transfer, these models get more complicated. For details it is therefore be referred to Wardenier (1982). |  |
| - Other types of joints made of CHS |  |
| - Related joints; - Plate to CHS connections; - Multiplanar joints. |  |
| - Related joints |  |
| The joint design resistance for the types of joints shown in Table 4 can be directly related to that for the basic type of joints in Table 2. |  |
| The joints a and c in the Table 4 have a similar loading effect as for an X-joint and the design resistance is therefore related to that for X-joints. |  |
| The joints b and d have a loading comparable to that for a K-joint and the design resistance is therefore related to that for K-joints. In all cases the brace load components perpendicular to the chord have to be considered, since these affect the chord yielding. It will also be clear that in the latter case the shear of the chord will be higher than for a K-joint and has to be considered separately. |  |
| - Design resistances of related joints (Wardenier 2002) |  |
| - Plate to CHS connections |  |
| Table 5 shows some joints with a circular hollow section chord and various configurations for the brace. In general, the design resistance for these types of joints can be related to each other by a general strength function: |  |
| - Design resistance of welded CHS joints with gusset plates (Wardenier 2002) |  |
| - Multiplanar joints |  |
| For multiplanar joints, two additional effects influence the joint capacity compared to that one for uniplanar joints: |  |
| - The geometrical effects (stiffening by the multiplanar joints); - The loading effects. |  |
| - Welded Connections between Rectangular Hollow Sections |  |
| The most economical and common way to connect rectangular hollow sections is by direct connection without any intersecting plates or gussets; this also gives the most efficient way for protection and maintenance. |  |
| The connections between rectangular hollow sections can be easily made, since the connecting members have to be provided with straight end cuts only. |  |
| Welded RHS connections: |  |
| - T-joints; - Y-joints; - X-joints; - K-joints (with gap and overlap); - N-joint (with gap and overlap); - KT-joint (with gap and overlap). |  |
| - Modes of Failure |  |
| The following modes of failure can occur: |  |
| - Brace effective width failure (tension brace or compression brace yielding); - Weld failure; - Lamellar tearing; - Chord face yielding; - Chord punching shear failure; - Chord side wall yielding or buckling; - Chord local buckling; - Chord shear failure. |  |
| - Failure modes for welded RHS connections (Wardenier 2002) |  |
| Only the following failure modes have to be considered in design, since local buckling can be omitted by choosing an appropriate cross section class, weld failure by welding with sufficient throat thickness and lamellar tearing by using materials according to the technical delivery standards (EN 10210 and EN 10219): |  |
| - Brace effective width failure; - Chord face yielding; - Chord punching shear; - Chord side wall failure; - Chord shear failure. |  |
| - Analytical Models for axial load connections made of RHS |  |
| For the determination of the influencing joint parameters, five models are used: |  |
| - Yield line model; - Punching shear model; - Brace effective width model; - Chord side wall bearing or buckling model; - Chord shear model. |  |
| - Yield line model |  |
| - Yield line model for a T, Y and X joint (Wardenier 2002) |  |
| For joints with medium b ratios the yield line model gives a good estimate of the chord face yielding capacity. |  |
| In principle, the yield line method is an upper bound approach. |  |
| The principle of the yield line method is based on equating the external energy by the external force N1 over a deflection d and the internal energy by the plastic hinge system with yield line lengths li and rotation angles i. |  |
| (per unit length) |  |
| Equating the sum to the external work gives: |  |
| This is a minimum for: |  |
| tanα=1−β |  |
| Substitution gives the capacity (T-,Y- and X-joints): |  |
| In this model, some simplifications have been incorporated, i.e. the thickness of the sections has been neglected (b – 2 t b). |  |
| The same applies to the weld sizes, which have not been incorporated. |  |
| For K-joints the load transfer is more complicated. |  |
| - Punching shear model |  |
| - Chord punching shear model for a T,Y and X joint (Wardenier 2002) |  |
| - Chord punching shear model for a K-gap joint (chord face) (Wardenier 2002) |  |
| Punching shear is caused by the brace load component perpendicular to the chord face, thus the punching shear criterion is given by: |  |
| For K-gap joints the gap size is extremely important for the effective punching shear length. |  |
| If the gap size is close to zero and the β value is low to medium, the gap part is relatively too stiff compared to the other perimeter parts. |  |
| Reduced effective length for punching shear. |  |
| For a large gap a similar situation occurs as for T, Y and X-joints, thus: |  |
| For a gap where the stiffness is about the same as at the sides of the braces, the punching shear criterion becomes: |  |
| Neglecting the thickness and the weld sizes, the gap here has to satisfy: |  |
| or |  |
| Due to the deformation capacity of the material, which has been proved experimentally, the limit can be extended to: |  |
| - Brace effective width model |  |
| - Brace effective width criterion for a T, Y and X joint (Wardenier 2002) |  |
| - Brace effective width criterion for overlap joints (Wardenier 2002) |  |
| For a T, Y and X joint, the effective width criterion can be given by (Figure 10): |  |
| For K-joints having a full effective cross wall of the brace at the gap (Figure 11), i.e.: |  |
| T, Y and X joints with a high  ratio generally fail by yielding or buckling of the chord side walls. |  |
| - Chord side wall bearing or buckling model |  |
| - Chord side wall failure model |  |
| T, Y and X joints with a high  ratio generally failed by yielding or buckling of the chord side walls, shown in Figure 12. The model used is similar to that used for beam to column connections between I-sections. For joints with    the capacity can be easily determined by: |  |
| For slender walls the yield stress fy0 is replaced by a buckling stress fk which depends on the chord web slenderness h0 / t0. |  |
| - Chord shear model |  |
| - Chord shear failure model (Wardenier 2002) |  |
| This model is based on the basic formulae for plastic design. |  |
| The plastic shear load capacity is given by: |  |
| with |  |
| Based on the Huber Hencky-Von Mises criterion the following interaction formula can be determined: |  |
| - Basic strength formulae |  |
| For T, Y and X joints up to β = 0,85, the yield line model for chord face yielding is used as a basic lower bound formula for the joint resistance. Above β = 0,85, the joint resistance is governed either by side wall failure, brace effective width or for b1 < b – 2 t – 2 by punching shear. |  |
| - Evaluation of the chord yielding for T, Y and X joints based on the yield line model (Wardenier 2002) |  |
| For K gap joints, a semi-empirical formula based on chord face yielding is used as the basic criterion. Depending on the joint parameters, various other criteria may become critical, e.g. brace effective width, chord punching shear or chord shear. |  |
| Due to the fact that in joints of rectangular hollow sections the sections can have different orientations and depth to width ratios, many configurations are possible, resulting in many failure modes and thus many strength formulae. |  |
| For K-joints with overlap, the basic joint strength criterion is based on brace effective width. If the b/t values are restricted, other failure modes will not be critical |  |
| - Evaluation to design rules |  |
| In principle, the evaluation to design rules, e.g. for K joints with gap, is similar as described for joints between circular hollow sections. |  |
| Since for T, Y and X joints for chord face yielding a lower bound yield line criterion is used, no statistical evaluation has been carried out. In more recent analyses based on numerical results, also a deformation limit (Yu et al 1993) is used for the ultimate strength and a full statistical treatment of the results has been carried out. |  |
| Table 7 shows the design resistance formulae for rectangular hollow section joints with the range of validity given in Table 8. |  |
| - Design resistance of welded joints between RHS (Wardenier 2002) |  |
| - Range of validity for welded joints between RHS (EN1993-1-8:2003) |  |
| - Joints loaded by bending moments |  |
| The design resistances are derived in a similar way as for the axially loaded joints. |  |
| To simplify the design, also here limitations are given for the range of validity to limit the criteria to be checked. |  |
| For Vierendeel girders it is recommended to choose joints with  = 1,0 to provide sufficient stiffness and strength. |  |
| - Other types of joints or other load conditions |  |
| - Joints between circular braces and a rectangular chord; - Joints between plates or I sections and RHS chords; - Multiplanar joints. |  |
| - Joints between circular braces and a rectangular chord |  |
| As far as chord face yielding concerns the joint strength of a joint with a circular hollow section brace di is about π / 4 times that of a joint with a square hollow section brace with a width bi = di, see Figure 15. This means that the same formulae can be used as for square hollow section joints, but they have to be multiplied by π / 4. This also means that the joints have the same efficiency, i.e. the joint strength divided by the squash load of the brace. |  |
| - Comparison of a K joint with a circular brace and an equivalent joint with a square brace (chord face) (Wardenier 2002) |  |
| - Joints between plates or I sections and RHS chords |  |
| These connections are approached in a similar manner as the rectangular hollow section joints and the same modes of failure have to be considered. |  |
| - Multiplanar Joints |  |
| Similar to circular hollow section joints, compared to uniplanar joints, multiplanar joints have a geometrical effect and a loading effect to be considered. |  |
| A multiplanar brace has a geometrical influence only if the β value is large, because then the chord side wall is stiffened.(see Figure 16). |  |
| - Multiplanar geometry effect for an XX joint of SHS (Wardenier 2002) |  |

- References

- Dutta, D., Wardenier, J. Yeomans, N., Sakae, K. Bucak, Ö., Packer, J.A. 1998. Design guide for fabrication, assembly and erection of hollow section structures. CIDECT Construction with hollow steel sections. TÜV Verlag Köln.

- EN 10210-1. 2006. Hot finished structural hollow sections on non-alloy and fine grain steels – Part 1: Technical delivery conditions: German version.

- EN 10210-2. 2006. Hot finished structural hollow sections on non-alloy and fine grain steels – Part 2: Tolerances dimensions and sectional properties: German version.

- EN 10219-1. 2006. Cold formed structural hollow sections of non-alloy and fine grain steels Part 1: Technical delivery conditions: German version.

- EN 10219-2. 2006. Cold formed structural hollow sections of non-alloy and fine grain steels Part 2: Tolerances, dimensions and sectional properties: German version.

- EN 1993-1-8. 2005. Eurocode 3: Design of steel structures – Part 1.8: Design of joints: German version.

- Kurobane, Y., Packer, J.A., Wardenier, J., Yeomans, N., 2004. Design guide for structural hollow section column connections. CIDECT Construction with hollow steel sections. TÜV Verlag Köln.

- Lu, L.H., de Winkel, G.D., Yu, Y. & Wardenier, J. 1993. Deformation limit for the ultimate strength of hollow section joints. In P. Grundy & A. Holgate & B. Wong (eds), Proc. intern. Symp. on Tubular Structures, Melbourne, 14-16 December 1994. Rotterdam: Balkema.

- Packer, J.A., Wardenier, J., Kurobane, Y., Dutta, D., Yeomans, N. 1995. Design Guide for circular hollow sections (CHS) joints under predominantly static loading. CIDECT Construction with hollow steel sections. TÜV Verlag Köln.

- Packer, J.A., Wardenier, J., Kurobane, Y., Dutta, D., Yeomans, N. 1992. Design Guide for rectangular hollow section (RHS) joints under predominantly static loading. CIDECT Construction with hollow steel sections. TÜV Verlag Köln.

- Wardenier, J. 1982. Hollow section joints. Ph.D. Thesis. Delft University Press, The Netherlands.

- Wardenier, J. 2002. Hollow Sections in Structural Applications. Bouwen met Staal, Zoetermeer, The Netherlands.