## Slide 2: Background (1)
When repeated fluctuating loading failure may occur before static resistance is exhausted.
Fatigue results from cracks starting from pre-existent micro- or macro defects and resulting in failure when section becomes insufficient to resist peak load.
In normal conditions cracks do not grow when stationary loading.
Buildings are normally not exposed to fatigue while bridges are.

## Slide 3: Background (2)
Welds are especially prone to such defects because of metallurgical discontinuities, rough weld profile and high residual stresses.
Weld toe
Crack
Weld toe
Cracks
Weld root
Butt weld (full penetration)
Mean stress
Actual stresses
Fillet weld

## Slide 4: Background (3)
In normal conditions cracks do not grow when stationary loaded.
In plain material the growth of a fatigue crack presents three successive stages:
  Initiation.
  Slow propagation.
  Sudden failure.

## Slide 5: Background (4)
Welded details are more questionable than plain material.
Crack growth rate found about proportional to , where a is its depth  A fatigue crack remains a small hardly detectable crack for most of its life .
In principle, only regions subjected to tensile stresses are susceptible to fatigue.
In practice, because of residual stresses, regions subjected to compressive stresses are checked to fatigue too.

## Slide 6: Background (5)
Once detected, cracks may be repaired.
Eurocode Part 1-9 is dedicated to fatigue design.
Assessment of fatigue resistance by means of fatigue strength curves for two types of details:
  Standard details applicable to nominal stresses.
  Reference weld configurations applicable to geometric stresses.
Fluctuating stresses are either direct or shear stresses.
Lecture focusing on CHS and RHS welded joints.

## Slide 7: Fatigue strength - Fatigue life (1)

max
min
mean
Number of cycles
Stress

max
min
mean
Constant amplitude stress range:
  Stress amplitude
  Fatigue life: number NR of cycles required to cause failure under given 
  Fatigue strength: R causing failure at given number N of cycles.

## Slide 8: Fatigue strength - Fatigue life (2)
Variable amplitude stress range:
  Spectrum over a representative period.
  Extrapolation to the expected service life of the structure.
  Spectrum  Histogram.
  Verification based on the concept of fatigue damage accumulation

## Slide 9: Fatigue damage accumulation (1)
Stress range: governing parameter.
Stress ratio: effect disregarded (due to residual stresses) except if stress relieved.
Constant amplitude stress range:
  No damage when < Constant amplitude fatigue limit.
Variable amplitude stress range:
  No damage when all < Cut-off fatigue limit.
  Damage given by Palmgren-Miner rule when some stress ranges or maximum stress range exceeds the constant amplitude fatigue limit.

## Slide 10: Fatigue damage accumulation (2)
Damage D = 1 means fatigue failure provided crack effects and service inspections are reflected appropriately through partial safety factors.
If histogram composed of k stress blocks of ni cycles with constant stress amplitude i:
Fatigue verification: D  1 ?

## Slide 11: Principles of fatigue resistance verification
Several types of methods:
  Of fundamental nature : Fracture mechanics.
  Of practical nature: Scope of EC3 Part 1-9:
    Classification method.
    Hot spot stress method.
Classification method:
  Applicable to constructional welded details (joints) classified in several categories with about the same fatigue life.
  Detail category  Nominal (constant amplitude) stress range for which the detail fails at 2106 cycles.

## Slide 12: Principles of fatigue resistance verification
Hot spot stress method:
  Also termed ‘geometric stress method’.
  Relates the fatigue life of a joint to the hot spot stress at the joint, i.e. the maximum geometrical stress where the crack is likely to be initiated (weld toe).
  Hot spot stress includes influences of geometry and type of load but excludes effects of fabrication (weld configuration) and local condition of the weld toe (radius, undercut, …).

## Slide 13: Partial safety factors (1)
In accordance with semi-probabilistic approach, partial safety factors Ff for fatigue loading and Mf factor for fatigue strength.
Fatigue loading determined based on fatigue loads with partial safety factor Ff = 1.
Partial safety factor Ff for fatigue strength depends on:
  Type of fatigue assessment.
  Degree of consequence of fatigue failure.

## Slide 14: Partial safety factors (2)
Partial safety factor Ff for fatigue strength:
(*) Satisfactory performance for specified design life under reservation of inspection and maintenance regime.
(**) Satisfactory performance for specified design life without need of regular in-service inspection.

## Slide 15: Design value of stress range (1)
Nominal stress range:
  For standard joints (esp. in tubular construction) listed in EC3 Part 1-9 (see Tables).
  Calculated at site of potential crack initiation.
  Effects of stress concentration accounted for through the fatigue strength.
  Design value:
Damage equivalent factor (see EC3) depending
on spectra and determined for N = NC = 2106 cycles
Corresponding to N = NC = 2106 cycles

## Slide 16: Design value of stress range (2)
  Constructional details :Hollow sections (t12,5 mm)

## Slide 17: Design value of stress range (3)
  Constructional details: Lattice girder node joints

## Slide 18: Design value of stress range (4)
Modified nominal stress range:
  When abrupt changes of sections close to site of potential crack initiation.
  Effects of stress concentration - other than those included yet in tables of constructional details - accounted for through stress concentration factor kf.
  Design value:

## Slide 19: Design value of stress range (5)
  When lattice girders: Simplified truss model with pinned connections may be used  .
  When lattice girders: Provided bending stresses due to load applied between the nodes are computed and accounted for, effects of secondary moments due to connection stiffness allowed for through magnification factor k1 (see Tables), so that:

## Slide 20: Design value of stress range (6)
k1 factor for CHS – In-plane loading
k1 factor for RHS – In-plane loading

## Slide 21: Design value of stress range (7)
Range for hot spot stress:
  When high stress gradients close to weld toe in joints listed in dedicated table.
  Detail categories of table are relative to crack initiating at toe of butt-welds, toe of fillet weld attachment and toe of fillet weld in cruciform joints.
Obtained from simplified truss model with pinned connections
Stress concentration factor
(see charts, esp. CIDECT Design Guide 8)

## Slide 22: Design value of stress range (8)
Detail categories for hot spot stress method

## Slide 23: Fatigue strength: Paris’ rule
Direct stress Shear stress

## Slide 24: Principle of S-N curves
C
D
L
Number of cycles
Direct stress range 
1
m1 = 3
m1 = 5
Cut-off limit
Constant amplitude fatigue limit
2106
5106
108
Detail category
Number of cycles
Shear stress range 
1
m2 = 5
Cut-off limit
Detail category
C
L
2106
108
D = 0,737 C
L = 0,549 D
L = 0,457 C
Note: m = 5 for 0 < N < 5106 cycles
for lattice girder node joints

## Slide 25: Typical S-N curves
Direct stress range 
Shear stress range 
Detail categories are given in previous tables

## Slide 26: Fatigue strength modifications (1)
Non-welded or stress relieved welded details in compression: few or no residual stresses  Less penalty of part of stress range in compression

## Slide 27: Fatigue strength modifications (2)
Some size effects due to thickness and other dimensional effects:
or apply possible recommendations given in previous Tables for some constructional details.

## Slide 28: Limit of applications of EN1993-1-9 Rules
Stress ranges (nominal, modified nominal, geometric) should not exceed:
Direct stress Shear stress

## Slide 29: Verification format (1)
Method 1- Comparison of action effects and fatigue strength:
Direct stress Shear stress

## Slide 30: Verification format (2)
Method 2 - Assessment of damage accumulation:
  Damage and endurance must incorporate the partial safety factors  for each stress block of the spectrum:
  i to be multiplied by Ff
         NR,i from S-N curves.
  C to be divided by Mf
  Cumulated damage during specified design life:

## Slide 31: Verification format (3)
Alternative to Method 2 - Equivalent constant amplitude stress range:
  Principle: Transform the design stress range spectrum (histogram) into an ‘equivalent’ constant amplitude design stress range equ so as to get same total Dd for a total number of cycles N = ni .
  Verification criterion:
with m = 3 or 5.

## Slide 32: Concluding remarks (1)
When repeated loads, fatigue is likely to produce cracks starting from local defects - such as especially welded details - and propagate till failure.
Fatigue resistance may prevail on static resistance.
Due to residual stresses, fatigue is checked in regions of tensile and compressive stresses.
Fatigue life of welded joints depends on type of joint, type of loading and structural detailing.
Partial safety factors apply both fatigue loading and fatigue strength.

## Slide 33: Concluding remarks (2)
Values of partial safety factors for fatigue strength depend on the type of fatigue assessment and the degree of consequence of fatigue failure.
Load spectrum is replaced by an accumulation of stress blocks with constant amplitude (histogram).
Damage is supposed to increase linearly with the number of cycles.
Total damage is obtained as the sum of partial damages relative to the individual stress blocks.

## Slide 34: Concluding remarks (3)
Fatigue life is supposed to be exhausted when the total damage reaches unity.
Two methods for fatigue resistance verification are given in EC3 Part 1-9 : the ‘classification method’ and the ‘hot spot stress method’.

## Slide 35: Concluding remarks (4)
When determining the stress range, due attention should be paid to additional stresses the effects of which are included neither in the fatigue strength, nor in the calculated stress range.
Depending on the situation, use is made of ‘nominal’ or ‘modified nominal’ or ‘geometric’ stress range.
Reference is made to typical fatigue strength curves for respectively direct stresses and shear stresses.

## Slide 36: Concluding remarks (5)
Detail category is the value of stress range C associated to an endurance of 2106 cycles.
Detail categories are given in EN1993-1-9 to most usual welded joints in hollow sections and welded nodes of lattice girders (note m = 5 for the latter).
Fatigue verification may be conducted based either on fatigue strength or on damage accumulation.